ADD:45REMIN ROAD(N) JISHOU, HUNAN, CHINA   Msn: fuyuqin@live.cn

TeL: 0086-743-8722840 Fax: 0086-743-8223336     E-Mail: fuyuqin@xiangximinmetals.com

Please note the picture of our product for Al-Mn-Tablets and the specs as follows:

|  |  | Number: | 4821524616 |
| --- | --- | --- | --- |
|  |  | Name: | Manganese Briquettes / Manganese Tablets / Manganese Alloys |
|  |  | Spec: |  |
|  |  | Memo: |  |
|  |  | Class: | Manganese alloy |

Product Readme

| ANALYSIS | ENGLISH | CHINESE |
| --- | --- | --- |
| Manganese | Percent: 75/80/85/90 | 锰含量:75%,80%,85%,90% |
| Aluminum | Percent: 25/20/15/10 | 铝含量:25%,20%,15%,10% |
| Size | Tablets overlaying stacked in cylindrical shape Diameter: 10-90 MM Height: 5-50 MM | 圆柱状 直径 10-90MM 高 5-50MM |
| Weight | 25g/200g/556g~1333g | 25克,200克, 556克~1333克 |
| Density | 3.7~403g/cm³ | 3.7~4.3克/立方厘米 |
| Colour Code | Silver grey Purple (AA colour code ) | 银灰色 (AA colour code) |
| Packing | Plastic shrink-wrap or foil wrapped rolls of 3~5 tablets each Packing in cardboard boxes 6 rolls each box (10 or 30 tablets/Box) | 塑料膜紧裹或金属箔片包裹成卷, 每卷3~5片, 每盒六卷 |
| Application | Tablets and mini-tablets are mainly focused to the aluminum industry for alloying application | 主要应用于铝合金生产工业 |